## Slide 1: Machine learning interatomic potentials for multicomponent systems
Konstantin Gubaev
Skolkovo Institute of Science and Technology (Skoltech)
Russia

## Slide 2: Motivation
What MD simulation is capable of doing?
Empirical potentials: 106 – 109 atoms, up to 1ms
Ab-initio models: 102 – 103 atoms, up to 1ps
Goal is to construct an interatomic potential:
Ideally: whose efficiency is comparable to the empirical, but accuracy is comparable to ab-initio.
At least: whose accuracy can be systematically improved at the cost of increasing computational complexity.
Construction of systematically improved potential

## Slide 3: Machine learning interatomic potentials
Problem statement
Picking of the training set | Selection of some representative set of configurations . Often experience-based
Training (finding optimal parameters of the model) | Solving the minimization problem:
Validation (checking accuracy of the model) | On a set , such as
Calculation of desired values (usage of the model) | 
Picking of the training set | 
Training (finding optimal parameters of the model) | 
Validation (checking accuracy of the model) | 
Calculation of desired values (usage of the model) | 

## Slide 4: Machine learning interatomic potentials
Partitioning scheme for energy of some configuration :
where is the neighborhood of the atom k
Atom interacts with its
neighborhood within some Rcut
Function is called
interatomic potential
Assumptions
Rcut
II
II
I
I
III

## Slide 5: Machine learning interatomic potentials
System energy:
Site energy:
Basis functions are scalar contractions of tensor moments:
Moment tensor potentials: functional form
Radial functions enumerated with µ
- fitting parameters
Tensor moments up to rank ν
- hyperparameters

## Slide 6: Machine learning interatomic potentials
Moment tensor potentials – radial functions
Radial functions depend on atomic species
They capture the “orbital configuration” between atomic pairs
- intense interaction
- weak interaction

## Slide 7: Machine learning interatomic potentials
Let
Examples of tensor moments:
(rank 0 tensor)
(rank 1 tensor)
(rank 2 tensor)
Examples of basis functions:
(scalar)
(scalar)
(scalar)
Moment tensor potentials - descriptors
– inertia tensor, invariant to translation, rotation and permutation of equivalent atoms
..., – atomic neighborhood

## Slide 8: Machine learning interatomic potentials
With ML potentials the error inside training domain is much lower, then outside
AL provides the numerical “measure of extrapolation” for a given configuration
AL allows to include only extrapolative configurations in the training set
Relies on the MaxVol algorithm
Active Learning

## Slide 9: Machine learning interatomic potentials
Each occurring configuration is either:
  Extrapolative, then we get a QM data for it
  Interpolative, then we provide for it
Learning on the fly

## Slide 10
Crystal structure prediction
Applications
Goal | Find the most stable alloys in a given composition range
Tools | Empirical selection of candidate structures Screening of the structures based on their energy
Success criteria | Locating of stable structures Experimental confirmation

## Slide 11
Crystal structure prediction
Usage of MTP
Applications
Relaxation via MTP (new configuration = termination)
Active selection of the training set from the relaxation trajectories
Retraining of the potential
Restarting the terminated relaxations

## Slide 12
Crystal structure prediction
AFLOW database*
Applications
Contains millions of structures
Relaxation is done with DFT
*Curtarolo S. et al. AFLOW: an automatic framework for high-throughput materials discovery //Computational Materials Science. – 2012. – Т. 58. – С. 218-226.

## Slide 13
Crystal structure prediction
Al-Ni-Ti convex hull
Applications
300 000 candidates* with 1-12 atoms (excl. 7,9,11)
Time consumed – 30 hours (~400 VASP calculations on 64 cores)
Result: most of the structures from AFLOW are found
*Samples were given by the group of Gus Hart from BYU

## Slide 14
Crystal structure prediction
Cu-Pd convex hull
Applications
40 000 initial candidates with different types of lattices and Pd content
Convex hull has FCC lattice on the edges and BCC lattice in-between
Result: all the structures from AFLOW are found

## Slide 15
Crystal structure prediction
Co-Nb-V convex hull
Applications
40 000 initial candidates with Co content higher than 50%
Result: the new structure is found, which is missing in AFLOW (Checked on VASP)

## Slide 16: Applications
Cheminformatics
Goal | Prediction of molecular properties based on their structure and composition
Tools | Machine learning models: Kernel methods Neural networks
Success criteria | Prediction accuracy Amount of input data required

## Slide 17: Applications
Cheminformatics
QM9 database*
130 000 organic molecules (С,H,N,O,F), each includes not more than 9 heavy (С,N,O,F) atoms
14 properties per molecule (we consider only enthalpy), computed at B3LYP/6-31G(2df,p) level of theory
Benchmark test for comparing of models in cheminformatics
*Ramakrishnan R. et al. Quantum chemistry structures and properties of 134 kilo molecules //Scientific data. – 2014. – Т. 1. – С. 140022.

## Slide 18: Applications
Accuracy (MAE, kcal/mol) provided by different models versus the Training Set size
Cheminformatics
Database QM9
(Training set + Validation set) – 130k molecules
Comparison of moment tensor model MTM ( = MTP) with the others:
For a 1 kcal/mol accuracy MTM requires not much data
Deep NNs are good for big training sets

## Slide 19
Cheminformatics
Active learning
Selection of optimal training set
Calculation of ab-initio data (not required in this case)
Retraining of the model
Accuracy check, move to step 1 or end
Active vs random picking: the maximal error is much lower with active learning
Applications

## Slide 20
Cheminformatics
Active learning
Applications
Active learning

## Slide 21: Summary
Parameterized interatomic potential for multicomponent systems (MTP)
Active learning algorithm
Interpolation of QM data
Prediction of the properties of metallic alloys and organic molecules
Running MD/relaxation with trained potential or learning on the fly
Big systems clustering ---> Large-scale modelling
(We cannot get QM data for large systems directly, thus we need to split them)
Key elements of the model:
Applications of the model:
Coming next:

## Slide 22: Thanks for attention! Any questions?
Contact me:
Konstantin.gubaev@skoltech.ru