## Slide 1: Dynamics of Skyrmions in Chiral Magnets
Charles Reichhardt, Cynthia Reichhardt, Dipanjan Ray, S.Z. Lin
Los Alamos National Laboratory

## Slide 2
courtesy of A. Saxena

## Slide 3
Tony Hilton Royle Skyrme, (1922–1987)
1961 Formulated a nonlinear field theory of massless pions in which particles can be represented by topological solitons
“Skyrmions”
1961-1984 Skyrmions generally ignored
Witten demonstrates connection between Skyrme’s model and QCD in the low-energy, large-Nc expansion.
2009 Experimental realization of skyrmions in chiral magnet (TMU)
T. H. R. Skyrme, Proc. R. Soc. London, Ser. A 260, 127 (1961).
: SU(2) field
Low energy effective field for QCD
Supports topological soliton, now known as skyrmion.
Skyrmions are realized in condensed matter systems, such as He3A, quantum Hall systems, Bose-Einstein condensates, multiband superconductors, liquid crystal and magnets.
Chiral Lagrangian
Stabilizing fourth-order term
Skyrmions

## Slide 4: Skyrmions in magnets
Spin configurations can wrap a sphere
Can have chirality
Spin shifts by p away from skyrmion core
Solitons in field theories with no massless fields: Vortices
Solitons in field theories with massless fields: Monopoles, skyrmions

## Slide 5: DM interaction: broken inversion symmetry
Example: Atomic crystal of (cubic B20) MnSi lacks space-inversion symmetry.
Result: Weak spin-orbit coupling
Generates slow rotations of all magnetic structures
Rotation scale: 190A; lattice constant: 4.56A.
Magnetic structures are effectively decoupled from atomic lattice.
Application of a magnetic field breaks time-reversal symmetry.

## Slide 6: First experimental observation
SANS
Bulk chiral itinerant-electron magnet:
MnSi
S. Mühlbauer, et al. Science 323, 915 (2009).
K . Kadowaki et al J. Phys. Soc. Jpn, 51, 2433 (1982)

## Slide 7: Direct visualization of magnetic structure
Lorentz Transmission Electron Microscopy
National Institute for Materials Science, Japan

## Slide 8: Real space observation of skyrmions in thin films
Helical
Skyrmion crystal
Close-up
X. Z. Yu et al. Nature 465, 901 (2010).
Lorentz transmission electron microscopy;
measure the in-plane component of spin.
Materials: Fe0.5Co0.5Si
Three-dimensional helical magnet
B30 w/ cubic but non-centrosymmetric structure

## Slide 9: Skyrmions have some similarities to superconducting vortices
B. Kalisky et al, PRB 83, 064511 (2011)

## Slide 10: In bulk samples, skyrmions are 3D objects
P. Milde et al, Science 340, 1076 (2013)

## Slide 11
Individual skyrmions can be created and destroyed
N. Romming et al, Science 341, 636 (2013)

## Slide 12: Driven skyrmions by current
Material:
Schulz, et. al., Nature Physics 8, 301 (2012).
Hall resistance is due to the emergent electric field induced by the motion of skyrmion.
The depinning current is extremely low. For magnetic domain wall .
Jonietz, et. al., Science 330, 1648 (2010).
Yu et. al, Nature Communications 3, 988 (2012).
Hall resistance measurement
Depinning current Jc ~ 102 A/c m2
Jc ~ 106 A/cm2

## Slide 13: Why Skyrmions are interesting
T. Schultz et. al., Nature Phys. 8, 301 (2012)
They can exhibit depinning transitions just like vortices; however, pinning is very low and skyrmions are very mobile
Similar to IV curve for vortex depinning
Can be manipulated by current => applications in spintronics, such as memory
Importantly, the threshold current to move a skyrmion is
104 to 106 [102 A/cm2] times smaller than that of magnetic domain wall. => less heating
Skyrmion velocity (2015) Beach group 8m/s 10^11A/m^2 room temperature

## Slide 14: Another reason for excitement: Huge potential for applications
Proposed skyrmion racetrack memory
Need to understand the dynamics and how to control with pinning, but no one knows.
High density memory
Novel low-dissipation logic devices
Can be driven with a low current density  Extremely low dissipation
Tremendous advantages over domain walls. Threshold current 105 or 106 less than that for domain wall
Once we understand skyrmion motion, sensing devices and hybrid structure can be constructed.
Fert et. al., Nature Nanotechnology 8, 152 (2013)
S. Z. Lin, C. Reichhardt and A. Saxena, Appl. Phys. Lett. 102, 222405 (2013)
Controlled creation and removal of skyrmion by a current pulse in a nanodisk

## Slide 15: Statics and Dynamics of Skyrmions May Have Overlap With Other Systems in Hard and Soft Condensed Matter
Colloids: Ideal system to study a variety of
basic problems in condensed matter systems
Vortices in superconductors, Bose Einstein condensates
Superconducting vortex lattice
Colloid Lattice (D Grier, NYU)
(JC Davis, Cornell)

## Slide 16: Can similar pinning effects occur for skyrmions ? Could one control the skyrmion lattice structure with pinning?
Pinning arrays can stabilize different types of vortex crystals and have commensurability effects.
There are already many known results regarding pinning vortices, manipulating them with structured landscapes, and a wealth of collective dynamics.
Harada et al
Kemmler et al, PRL 2006

## Slide 17: Continuum model for skyrmions
We consider a 2D chiral magnetic film w/ Dzyaloshinskii-Moriya interaction, w/ Hamiltonian
where Jex: exchange interaction, D: spin-orbit DM interaction, B: external field, A: Anisotropy, n: unit vector. Equation of motion for spin: Landau-Lifshitz-Gilbert equation
where the last term is the spin transfer torque with the external current.
The number of skyrmions is given by the topological number
ferromagnetism
Skyrmion
Spiral
First order phase transition
Phase diagram at
Upon increasing the magnetic field, the skyrmion density first increases and then drops.
dtn=-gnxHeff – anxdtn – (J.∇)n
With Heff=-dH/dn=Jex ∇2n – 2D∇xn + B + JAnzz

## Slide 18
Magnetic spiral structure at small B
Triangular lattice of skyrmions at intermediate B
S.Z. Lin, C. Reichhardt, C.B. Batista, A. Saxena, PRL 110, 207202 (2013)

## Slide 19: Dynamic phase diagram for chiral magnet: No pinning
In the spiral phase, if one applies strong current, the spiral structure becomes unstable and evolves into skyrmion lattice.
In skyrmion phase, the IV is linear and the slope depends on the number of skyrmions.
S.Z. Ling, C. Reichhardt, C.B. Batista, A. Saxena PRL 110, 207202 (2013)

## Slide 20: Can we make a particle-based model for skyrmion dynamics?
b=2/x2=2HaJex/D2
Proportional to applied field and exchange energy
Inversely proportional to spin-orbit coupling
External field induces a spin wave excitation gap, so that spins in skyrmion tail recover exponentially to fully polarized state.
The interaction between two skyrmions is short-ranged
F~K1(r/x) with x=(D2/JexB)0.5, similar to vortex

## Slide 21: Skyrmion Particle-based model
Equation of motion
a: damping constant
b: Magnus term strength
Fss: isotropic skyrmion-skyrmion repulsion
Fsp: skyrmion pinning force
Fd: external drive

## Slide 22: Magnus Force Effects Dynamics
Magnus force is responsible for the weak pinning of skyrmions
S.-Z. Lin, C. Reichhadt, Batista, PRB (2013)
Similar conclusion obtained by continuum model:
Iwasaki et al., Nature Communication 4, 1463 (2013)
Comparison between the continuum and particle-model

## Slide 23
b/a=0 Fd=0.20
b/a=10 Fd=0.05
b/a=10 Fd=0.20
Overdamped limit
Particle trajectories through an attractive pinning site for a vortex vs a skyrmion
Vortex limit
Skyrmion
C. Reichhardt, D. Ray, and C.J. Olson Reichhardt PRB (2015)

## Slide 24
b/a=10. Fd=0.05. Fp=0.10.
Pinning induced side-jump effect on skyrmion motion, implies that pinning or disorder will
affect the measured Hall angle.

## Slide 25
Skyrmion motion shows much more winding orbits

## Slide 26
J. Iwasaki, M. Mochizuki, N. Nagaosa, Nature Nanotechnol. 8, 742 (2013)
Skyrmion velocity-force curves also observed in other continuum simulations

## Slide 27
F. Pardo et al, Nature 396, 348 (1998)
C.J. Olson et al, PRL 81, 3757 (1998)
Vortices in the presence of quenched disorder can exhibit elastic or plastic depinning and can undergo dynamical reordering transitions in the moving state.
A. Koshelev and V. Vinokur, PRL (1994).

## Slide 28: Drive in x direction, Elastic Depinning, Skyrmions move as a Lattice
R = Vy/Vx
Hall angle changes with drive
Particle-based simulation of elastic depinning

## Slide 29
Skyrmion velocity vs force curves in the presence of random pinning: Dynamical
reordering transition, Hall angle depends on drive.
C. Reichhardt, D. Ray, and C.J. Olson Reichhardt PRL in press

## Slide 30
Dynamic phase diagram: MC moving crystal, ML moving liquid, PC pinned crystal,
PG pinned glass, No moving smectic state due to Magnus term
C. Reichhardt, D. Ray, and C.J. Olson Reichhardt, PRL in press

## Slide 31
Pinned skyrmion crystal
Pinned skyrmion glass

## Slide 34: Quench on random disorder from triangular lattice
Increasing
Magnus
term

## Slide 35: Dynamic Reordering of Skyrmions
Disordered skyrmions reorder at higher drives than vortices,
but order into a crystal rather than a moving smectic as for vortices
Fraction
of particles
with six neighbors

## Slide 36: Structure Factor S(k) for Driven Skyrmions
Fd = 0.0
Pinned skyrmion
glass
Fd = 0.5
Moving liquid
Fd = 1.0
Moving liquid
Fd = 4.0
Moving crystal
C. Reichhardt, D. Ray, and C.J. Olson Reichhardt PRL in press

## Slide 37: Structure Factor S(k) for Driven Vortices
Fd = 0.0
Pinned
vortex
glass
Fd = 0.5
Moving liquid
Fd = 2.0
Moving liquid
Fd = 4.0
Moving smectic

## Slide 38
Skyrmion density
I
I
V
Periodic pinning potential
Commensuration effects
Asymmetric pinning potential:
Skyrmion diode/ratchet
Guided skyrmion motion
I
V
Transverse motion
Longitudinal motion
Controlling skyrmion motion with patterning: for applications and for new basic science of skyrmions

## Slide 39: Periodic pinning structures with changes in local anisotropy
Commensurate
Incommensurate
1D Periodic

## Slide 40: Vortex motion can be controlled with asymmetric structures: Vortex ratchets
An ac drive induces a dc motion of the vortices. Could something like this be done for skyrmions?
B. Plourde, Syracuse
J.E. Villegas et al, Science 302, 1188 (2003)
C.C. de Souza Silva et al, Nature 440, 651 (2006)

## Slide 41: Skyrmion on a quasi-1D asymmetric substrate with ac drives parallel or perpendicular to substrate asymmetry
C.S. Lee et al, Nature 400, 337 (1999)
V.A. Shklovskij, O.V. Dobrovolskiy, PRB 84, 054515 (2011)
I. Guillamon et al, Nature Physics 10, 851 (2014)

## Slide 42: AC driving in parallel direction. Red-Parallel, Blue-Perpendicular

## Slide 43
Phase diagram of ratchet effect for AC driving in parallel direction

## Slide 44
AC driving in perpendicular direction. Magnus induced ratchet effect

## Slide 45
Ratchet orbits for AC driving in the perpendicular direction
n = 1
n = 2
n = 0
n = 2

## Slide 46: Ratchet dependence on Frequency
Perpendicular AC
Parallel AC

## Slide 47: Magnus-induced trajectory shift upon passing through pinning site
b/a=0
b/a=1
b/a=10

## Slide 48: Negative differential conductivity observed for vortices moving in periodic defect arrays
C. Reichhardt et al, PRL 78, 2648 (1997)
Experiment
Simulation
J. Van de Vondel et al, PRB 79, 054527 (2009)

## Slide 49: Single skyrmion moving in square pinning array: Varied Hall angle
Vortex case

## Slide 50: Changing Hall angle = changing skyrmion orbit

## Slide 51: Changing Hall angle = changing skyrmion orbit

## Slide 52
Quantized
Hall angle

## Slide 53: Comparison between skyrmions and vortices in type II superconductors
 | skyrmions | vortices
Homotopy class | : | :
Emergent EM fields | Yes | No
Thermodynamic phase | Triangular lattice | Triangular lattice
Current drive | In metals yes | yes
Equation of motion | Mangus force dominates | Dissipative force dominates
Pinning | Weak | Strong
Unstable at high current drive | Yes | Yes
Magnetoelectric coupling | In insulators yes | No

## Slide 54: Future
Skyrmion transformers
Skyrmion jamming
Skyrmion mass: shock waves, nonlinear waves, phonon modes in skyrmion crystals?

## Slide 55: Future: Single skyrmion manipulation similar to that achieved for vortices
O. Auslaender et al, Nature Physics 5, 35 (2009)

## Slide 56: Conclusions
Continuum skyrmion model captures known phases
We construct effective pairwise skyrmion-skyrmion and skyrmion-defect interaction potentials.
Interaction of an assembly of particles with Magnus force and quenched disorder has never been explored.
Skyrmions interacting with periodic or random pinning exhibit rich features in the velocity-force curves, including Hall response and negative differential resistivity.
Experiments on skyrmions are in their infancy. Field can benefit from what is already known about vortex transport, such as controlled pinning for skyrmions.